## Slide 1
Magnetic Micro-Calorimeters
for atomic and nuclear physics
Andreas Fleischmann, Loredana Gastaldo, and a large team at
Heidelberg University
New perspectives in the charge radii determination for light nuclei
ECT* Workshop, July 2025, supported by

## Slide 2: micro-calorimeters
Operation at low temperature (T < 0.1 K):
small specific heat
large temperature change
small thermal noise !
Temperature change
Relaxation to bath temperature
Thermal bath (T < 100mK)
Weak thermal link G
Absorber C
Thermometer
X-ray photon or particle
Thermal detectors !
Somewhat numb: Convert good form of energy to heat!

## Slide 3: metallic magnetic calorimeters
paramagnetic sensor: Au:Er500ppm , Ag:Er
main differences to resistive sensors like TES and thermistors
no dissipation in the sensor
no galvanic contact to the sensor
M and C of weakly interacting spins well understood
signal size:
numerical optimization
non-linearity: small & understood from thermodynamics
important for large arrays
t
T
~1 mK
20 mK
~1 ms
M
T

## Slide 4: thermodynamical properties of Au:Er, Ag:Er
Au:Er 300 ppm
Inverse Temperature T1 [K 1]
Magnetization M [A/m]
Au:Er 300 ppm
Temperature T [mK]
Specific heat C [104 J mol1K1]
Au:Er 300 ppm
signal size can be predicted with confidence
non-linearity as well !
RKKY-interaction between Er-spins ~ 3 times stronger in silver
electrons
thermodynamic properties of interacting spins are well understood
typical range of operation

## Slide 5: detector geometries
planar paramagnetic T-sensor
superconducting pickup loop with persistent current to generate bias B-field
250 mm
meander-shaped pick-up coil
stripline (sandwich) design
filling factor ≈ 0.4
filling factor ≈ 0.8

## Slide 6: two-stage dc-SQUID setup
300K
main advantages:
low readout noise
large system bandwidth (several MHz)
low power dissipation (close to the MMC)
linearization by flux locked loop
< 100 mK
input coil should
match pickup coil

## Slide 7
microwave SQUID multiplexer (µMUX)
readout 100s of pixels with only one HEMT amplifier and two coaxes

## Slide 8: micro-fabricated devices: first 1×8 array for soft x-rays (a decade ago)
1×8 x-ray absorbers
  250μm×250 μm gold, 5 μm thick
  98% qu.-eff. @ 6 keV
  electroplated into photoresist mold
  mech/therm contact to sensor by stems to prevent loss of initially hot phonons
Au:166Er300ppm temperature sensors
Superconducting meander shaped pickup coils
  2.5 μm wide Nb lines
  Ic ≈ 100mA
On-chip persistent current switch (AuPd)
250 mm
Au:Er
on
Nb meander

## Slide 9: signal rise in compact x-ray detectors
rise time: 90 ns @ 30 mK, as expected for the electron-spin-relaxation of Er in Au

## Slide 10: signal decay
decay time
adjusted by metallic thermal link (Au)
here: 3 ms @ 30 mK
On-chip thermal bath
magnetic flux
time

## Slide 11: first 1×8 array for soft x-rays
DEFWHM = 1.6 eV @ 6 keV
DEFWHM = 1.5 eV @ 0 keV
55Mn
Defines state-of-the-art together with TES from NIST and NASA

## Slide 12
8×8 arrays of maXs-1/20/30/200
1.2/2/4/8 mm
Dry dilution fridge
(Bluefors, FI)
8 × 8 pixels for photons up to 1/20/30/100 keV with DEFWHM = 0.5/2/5/30 eV
highly symmetric design -> cross-talk

## Slide 13
maXs-30
maXs-30 mounted on coldfinger of a dry dilution fridge

## Slide 14: maXs-30
T

## Slide 15
maXs-30 an 8×8 pixel array for x-rays up to 30 keV
Absorbers:
each 0.5mm × 0.5 mm
30-50 mm thick gold
9.8 eV
Energy resolution ΔEFWHM = 9.8 eV @ 59 keV
Resolving power: 6000 (limited by gain drifts)

## Slide 16: 233U + 241Am spectrum
229Th
229Th
Many high-statistics lines → Allows broadband calibration
Co-added 20 channels, several weeks of data taking
Notes: I want to start the talk .. Showing our wide-range spectrum of …. From 20 channels

## Slide 17: maXs-30: calibration
non-linearity
non-linearity as thermodynamically expected!

## Slide 18: maXs-30: present calibration residuals
Most lines from literature have too large uncertainty.

## Slide 19: maXs-30: present calibration residuals
Sub-eV agreement for carefully selected calibration lines.
Left-over residuals due to ADCs  sparse set of calib.-lines should allow for ppm-level (FS) calibration

## Slide 20: Effects of ADC non-linearity scaled to the Lamb-shift / QUARTET-experiment (worst case)
Presently used digitizers: Struck SIS3316 (AD9268)
16 bit for +/- 120 keV (1 LSB = 3.7eV)
„no missing codes“, i.e. bits are up to ± 0.5 LSB off: 1 → 0.7
2 → 2.1
4 → 3.6
8 → 8.2
…

## Slide 21: Effects of ADC non-linearity
16 bit for +/- 120 keV
„no missing codes“, i.e. bits are up to ± 0.5 LSB off: 1 → 0.7
2 → 2.1
4 → 3.6
8 → 8.2
…

## Slide 22: Effects of ADC non-linearity
16 bit for +/- 120 keV
overall nonlinearity for processed, simulated pulses:

## Slide 23: Effects of ADC non-linearity
16 bit for +/- 120 keV
overall nonlinearity for processed, simulated pulses:

## Slide 24: Measured ADC non-linearity
16 bit for +/- 60 keV
measured non-linearity of SIS-3316:

## Slide 25: Effects of ADC non-linearity on energy calibration
16 bit for +/- 60 keV
based on measured non-linearity of SIS-3316.
pulses average over large voltage ranges removing errors of small bits

## Slide 28: MMCs get more and more mobile
here @ entrance to Frejus tunnel between Italy and France

## Slide 29
Two maXs-100 systems @ e-cooler of CRYRING @ GSI/FAIR: He-like Uranium
Beamtimes 2021 & 2025

## Slide 30
maXs-30 @ -beamline, PSI: muonic Li, B, C

## Slide 31: summary & outlook
metallic magnetic calorimeters combine in a unique way
energy calibration: sparse set of calibration lines will allow for ppm-FS-accuracy for line-positions in fullrange
micro-fabrication works
scaling to pixelcounts > 100 in progress
large variety of sizes, stopping powers and resolutions
MMCs start to contribute to atomic, molecular, nuclear and astro-particle physics
time resolution
energy resolution
linearity

## Slide 32
maXs-30 @ -beamline, PSI: muonic Li, B, C

## Slide 33
maXs-30 @ -beamline, PSI: muonic Li, B, C

## Slide 34
first broadband hi-res spectrum of muonic 6Li and 7Li
2p – 1s
3p – 1s
4p – 1s
preliminary

## Slide 35
first broadband hi-res spectrum of muonic 6Li and 7Li
2p – 1s
3p – 1s
4p – 1s
preliminary
isotope shift resolved

## Slide 36: MOCCA: 4k-pixel molecule camera
to study reaction cross sections of molecular ions of cold interstellar plasmas
in the cryogenic storage ring CSR at MPI-K, HD
MOCCA:
44.8mm × 44.8mm
64 × 64 pixels
resolution: DE = 250 eV (FWHM)
operated at T = 20 mK
16 two-stage SQUIDs to read-out 64 rows
16 two-stage SQUIDs to read-out 64 columns
Heidelberg University, MPI-K Heidelberg, Columbia Astro Lab NY
Position and energy resolved detection
of neutral molecular fragments
after neutralizing with an electron in the e-cooler
T < 10K

## Slide 37: MOCCA: 4k-pixel molecule camera / hi-res alpha detector
45 mm
200 eV FWHM